BONDACRYL VOLUME CHART

Mix for floor to wall joints/patch repairs to concrete floors

| HOLE VOLUME | ORDINARY PORTLAND CEMENT (KG) | WASHED, SHARP SAND (KG) | BONDACRYL |
| --- | --- | --- | --- |
| 1 LITRE | 0.4 | 1.6 | 0.15 LITRES |
| 10 LITRES | 4 | 16 | 1.5 LITRES |
| 20 LITRES | 8 | 32 | 3 LITRES |
| 50 LITRES | 20 | 80 | 7.5 LITRES |

Material required per metre length for floor to wall joints

| JOINT WIDTH & DEPTH (VOLUME PER METRE) | BONDACRYL LITRES | ORDINARY PORTLAND CEMENT (KG) | WASHED, SHARP SAND (KG) |
| --- | --- | --- | --- |
| 25mm x 25mm (0.625 Litre) | 0.094 | 0.25 | 1.00 |
| 50mm x 50mm (2.5 Litre) | 0.375 | 1.00 | 4.00 |

COVERAGE FOR SIZES AVAILABLE

| BONDACRYL | ORDINARY PORTLAND CEMENT (KG) | WASHED, SHARP SAND (KG) | HOLE VOLUME |
| --- | --- | --- | --- |
| 1 LITRE | 2.67 | 10.66 | 6.66 LITRES |
| 2.5 LITRES | 6.68 | 26.65 | 16.65 LITRES |
| 5 LITRES | 13.35 | 53.3 | 33.3 LITRES |
| 25 LITRES | 66.75 | 266.5 | 166.5 LITRES |

DCM/06/08